## Slide 1: A Sustainable Planet
Week 5
Formation of mineral resources
Dr Vicky Coker
Department of Earth and Environmental Sciences
vicky.coker@manchester.ac.uk; Williamson Building

## Slide 2: Learning outcomes
Understand the necessity of mining metals
Explain how geological processes lead to ore deposit formation
Identify some key geological settings for ore deposits
Explain the mineralogy of some key ore deposits
Explain how some key metals are refined
Explain critical minerals and their supply risks
2024 status: Stagnation
2024 status: Stagnation

## Slide 4: Contributions of raw materials to SDGs
European Commission: Joint Research Centre, Grassi, G., Mancini, L., Vizzarri, M., Wittmer, D. et al., Mapping the role of raw materials in sustainable development goals – A preliminary analysis of links, monitoring indicators and related policy initiatives, Publications Office, 2019, https://data.europa.eu/doi/10.2760/026725

## Slide 5: Plate tectonics and resources
Lithospheric plates move due to mantle convection
Convergent and divergent plate boundaries lead to differing deposits of earths resources
Particularly:
  Mid-Ocean-Ridges
  Subduction Zones

## Slide 6: Tectonic Environments

## Slide 7: Processes of Ore Formation
Enrichment of OFEs (ore forming elements) above background concentrations
Geochemical Perspectives, vol. 6, p18

## Slide 8: Ore Formation – Precipitation from Mobile Fluids
Source
  Selective extraction from source rock into a mobile phase
Transport
  Transport to the site of deposition
Deposition/precipitation
  Ore minerals precipitated into a comparatively small volume of rock

## Slide 9: Aqueous Fluids
Most important ore-forming fluid
  Capacity for solubilising metals
  Capacity for transporting Ore Forming Elements & heat
  Precipitate metals in response to chemical gradients
    T (temperature)
    P (pressure)
    X (fluid composition)
  Often through acid/base or redox reactions

## Slide 10: Ore Forming Fluids
Rock melts
Aqueous fluids
  Magmatic exhalations
  Regional metamorphic fluids
  Meteoric hydrothermal fluids
  Surface/near surface waters
Mafic Fe-Ti
Ni-Cu Sulfides
Porphyry Coppers
Skarns
Archean Gold Lode Deposits
Volcanic Massive Sulfides
Deposits
Mississippi Valley Type
Deposits
Precambrian BIF Deposits
Sandstone-hosted uranium

## Slide 11
Many common rocks contain significant amounts of “abundant metals” but only a few are rich enough to be mined as “ores”
Note: Factors important are:
mineralogy
grade
grain size/texture
size and depth of deposit
geographic location
possible by-products
Mineralogy and grade are particularly important: only some minerals are rich enough in the metal to be “ore minerals”
e.g.: Iron easier to remove from Fe2O3 than from Fe2SiO4
Size/depth/geographic location influence mining and transport costs
Mineralogy, grain size, texture influence process methods/costs
By-products can add to value

## Slide 12: Critical materials
Availability
Production as a by-product
Demand
Low substitutability
Virtually no recycling
High supply risk

## Slide 13: UK critical minerals 2024
UK 2024 criticality assessment
Notes: UK 2024 criticality assessment

## Slide 15: Iron

## Slide 16
Mineralogy dominated by iron in two oxidation states
FERROUS (Fe2+):
relatively soluble
forms minerals such as:
Siderite (FeCO3)
Chamosite (Fe(Si,Al)2O5(OH)4)
FERRIC (Fe3+):
relatively insoluble
forms minerals such as:
Hematite (Fe2O3)
Goethite (FeOOH)
Iron Deposits can form through igneous, metamorphic or sedimentary processes
Chamosite
Siderite
Hematite
Goethite

## Slide 17: Residual Deposits-Laterite formation
Soils rich in Fe that form in hot, wet subtropical and tropical environments
Laterite –source of iron and nickel
Created through weathering a soil under strong oxidising and leaching conditions
Chemical weathering removes the more soluble material and leaves Fe hydroxides -Fe(OH)3
Laterite-can be used as a building material
Laterite formation

## Slide 18: Sedimentary Deposits
Three types:
1) Bog Iron Deposits
Small, no longer mined but historically important
Fe mobilised as Fe2+ in swamps (“bogs”)
Transported in organic–rich near–surface waters
Enter oxygen–rich lake (or coastal waters) oxidize to Fe3+ and precipitate
Ore: Goethite (FeOOH) and magnetite (Fe3O4)

## Slide 19
2) Ironstones
Continuous sedimentary beds – extend 100’s km
Mostly shallow near-shore marine sediments
  Shallow-oxidising Ores:Goethite, hematite
  Deeper-more reducing- Ores: siderite and chamosite
Iron transported in fluids and replaced calcium carbonate, fossils or oolites
Phanerozoic-type deposits
Goethite ooids in an ooidal ironstone (Lr Jurassic)
Musselband Ironstone-non-marine bivalve, Scotland

## Slide 20: 3) Banded Iron formations (BIFs)
Bulk of the worlds iron ore reserves
Grade 30-50% Fe
Occur only in Precambrian rocks 1.8-3.8 billion years ago
Large: 30-700m thick and can be 1000’s km extent

## Slide 21: BIFs: mineralogy and origin
Origin is somewhat enigmatic
Marine basin setting
Runoff from continents of Fe2+ rich weathering and erosion material also from submarine hydrothermal fluids
Free oxygen was rare or absent on the Precambrian Earth
Oxygen (produced by cyanobacteria or photoferrotrophs) was combining with abundant iron in oceans of the early Earth to form BIFs
Formation of abundant BIFs stopped once the atmosphere contained more oxygen from bacterial photosynthesis
Fine-grained magnetite/ hematite with quartz, Fe silicate and Fe carbonate minerals
Later metamorphosis of most due to age
Possible model for BIF deposition
Deformed BIF

## Slide 22
Schematic diagram showing the relative abundance of Precambrian BIFs vs. time, with several of the major BIFs or major BIF regions identified.
Global occurrence of Precambrian BIFs. The map emphasizes the wide distribution of BIF and shows only a selection of well-known occurrences of different ages and kinds.

## Slide 24: Steel making
Blast furnace processes

## Slide 25
World Steel Association

## Slide 26: Summary -Fe
Worlds reserves are widespread and critical to the steel industry
2.3+ million metric tons of iron ore produced per year
3rd most abundant element
Deposits formed through igneous, sedimentary and metamorphic activity
Main ore minerals are magnetite and hematite
Main ore deposit are Banded Iron Formations (BIFs) which are Precambrian in age

## Slide 27: BATTERY ELEMENTS

## Slide 28: Learning outcomes
Explain Li-ion battery technology
Discuss key battery elements:
  Manganese
  Aluminium
  Nickel
  Copper
  Cobalt
  Lithium
Geological settings of ore deposits
Mineralogy of ore deposits
Production of the pure material

## Slide 29
UK: All new cars and vans will need to be 100% zero emission by 2035. And no new petrol or diesel cars will be sold after 2030
UK Government (DfT) December 2024

## Slide 30
But what is in an electric car battery?
https://www.nature.com/articles/d41586-021-02222-1

## Slide 31: Batteries
Layered lithium cathode material is key
Added:
  Nickel increases energy density but decreases stability
  Cobalt helps stabilise the Ni
  Manganese and Aluminium can also help stabilise Ni but not as effectively
Use copper and aluminium collectors to cycle charge

## Slide 32
https://www.benchmarkminerals.com/

## Slide 33: Manganese
Crustal abundance 0.095%
90% of mined manganese used in the iron and steel industry
Mn added to smelting as ferromanganese
  Scavenger of impurities e.g. sulfur and oxygen
Water treatment and purification
Key component of a lithium cathode battery

## Slide 34: Mn chemistry and minerals
Exists in nature in different oxidation states
Minerals
Rhodocrosite
MnCO3
Psilomelane
BaMn9O18.2H2O
Pyrolusite
MnO2

## Slide 35: Sediment-hosted Mn ore deposits
Notes: Manganese ore deposits, all dating from the Oligocene, form an arc around the north side of the Black Sea, stretching from Turkey through Bulgaria, the Ukraine, Russia and Georgia and finally in Kazakhstan. They constitute the third great episode of Mn deposition, in the Early Oligocene.
Black Sea deposits (click for larger image). Not shown is Mangyshlak in Kazakhstan.
Table of average ore compositions
These and most other large Mn deposits likely formed around the margins of euxinic basins (those with free H2S in deep water). Such basins -- exemplified by the modern Black Sea -- have a thin zone of oxygen-containing water overlying a large reservoir of oxygen-free, sulfidic water. Elements like Mn that are soluble under reducing, sulfidic conditions but insoluble under oxidizing conditions precipitate along the interface between these water masses. Generally the Mn solids simply sink back into the sulfidic water and redissolve, but along basin margins, where the transition impinges on the bottom, Mn oxide accumulates in the bottom sediment where it reacts with organic matter to form Mn carbonate (Force and Cannon,1988; Okita, 1987; Okita et al. 1988; Maynard et al., 1990; Okita 1992, and Okita and Shanks, 1992).
The overall process can be represented schematically by the reaction
2MnO2 + CH2O + HCO3- → 2MnCO3 + H2O + OH- .
1/2 the C incorporated in the MnCO3 comes from organic matter, which has an isotopic composition of ~ -27 permil, while the remaining 1/2 comes from oceanic HCO3 with an isotopic composition close to 0 permil.
The resulting Mn deposit will have a good correlation between Mn grade and d13C with high grade samples approaching -15 permil.
http://www.sedimentaryores.net/Manganese/Black%20Sea%20index.html

## Slide 36: Ferromanganese nodules
For Mn-nodules need:
low sediment rates
constant flow of water
good O2 supply from ocean circulation
aqueous sediments –pore waters=diagenetic nodules
Slow growing 1mm in 1000 years

## Slide 37
A source of critical metals
-Rare Earth Elements

## Slide 38: Aluminium
2nd most abundant metal -8.2% of crust
Weighs only 1/3 that of iron or copper
Useful properties to make it easy to machine and cast
  Corrosion resistant
  Conductor of electricity
Wide number of uses

## Slide 39: Bauxite
Soils rich in Al that form in hot, wet subtropical and tropical environments
Bauxite -aluminium ore
Pisolitic texture
Most deposits are younger than 60 million years
Can extend laterally over large areas
Enriched in Al to ~35%

## Slide 40
Chemical weathering removes the more soluble material from aluminium-silicate rocks and leaves a residue of:
  Al hydroxides
    Gibbsite Al(OH)3 –primary mineral in lateritic bauxite -tropics
    Boehmite g-AlO(OH) – primary mineral in karst bauxite-Europe
    Diaspore a-AlO(OH)
  Clays e.g. Kaolinite Al2Si2O5(OH)4
  Fe oxides
  Created through weathering a soil under strong oxidising and chemical leaching conditions-lateritic weathering
+Aluminium

## Slide 41
Notes: Crushing: Bauxite ore is crushed, washed, and dried.
Digestion: The bauxite is heated in a caustic solution, usually sodium hydroxide, at high temperatures and pressures.
Separation: The hot sodium aluminate slurry is separated from the undissolved residue, called "red mud".
Precipitation: Aluminum hydroxide is precipitated from the hot solution by adding aluminum hydroxide seeds.
Separation again: The aluminum hydroxide is separated from the spent caustic liquor.
Washing and drying: The aluminum hydroxide is washed and heated to remove excess water.
Calcination: The aluminum hydroxide is heated to form alumina.

## Slide 42
Requires 950°C, 150,000A and 1000V for metal reduction from the cryolite

## Slide 44: Nickel
Nickel improves durability and corrosion resistance of steel
Ni depleted in the earths crust – 0.0072% Ni
Mafic and ultramafic igneous rocks transport Ni from the mantle- 0.1% Ni
Present in olivines and pyroxenes-substitutes for Mg and Fe
http://www.roskill.com/

## Slide 45: Sulfide-Nickel Deposits
http://pubs.usgs.gov/info/mwni_cu/
Pentlandite (yellow-white) (Fe,Ni)9S8
Pyrrhotite (pink-brown)
Fe7S8

## Slide 46: Sudbury, Ontario
Ni deposits formed through magmatic segregation
56 km x 26 km elliptical deposit
Conical shape-due to meteor impact
Magmatic fluids used the fractures formed during the impact to form the deposit

## Slide 47: 2-Residual deposits
Chemical weathering of mafic and ultramafic rocks
Hot, humid subtropical conditions
Silicates breakdown to form hydrous compounds
Ni-rich laterites
Representation of “Residual Weathering Model”
Garnierite (H2(Ni,Mg)SiO4

## Slide 48: Nickel production
Massive sulfide deposits: Canada, Russia and Australia
Large laterite nickel deposits: Cuba, New Caledonia, Indonesia

## Slide 49: Processing
https://www.smm.co.jp/en/business/nonferrous/

## Slide 50: Copper
High electrical conductivity
Easily joined and soldered
Common ore minerals include:
  Chalcopyrite CuFeS2
  Bornite Cu5FeS4
  Enargite Cu3AsS4
Chalcopyrite
Bornite
Enargite

## Slide 51: Tectonic setting
Three types of deposit:
  Magmatic segregation
  Hydrothermal deposits
  Sediment-hosted stratiform deposits
http://www.geo.fu-berlin.de/fb/e-learning/geolearning/en/mountain_building/resources/porphyry_copper_ore_deposits/index.html
http://geology.com/usgs/uses-of-copper/
Porphyry copper deposits
HYDROTHERMAL DEPOSITS

## Slide 52: Porphyry copper
Intrusive magma- containing ~4% water
A crust forms around the edge of the intrusion as it cools
As the rising magma cools the hot water is released
Pressure increases, steam explosions shatter the overlying rock
Escaping hydrothermal solutions carrying ore metals more along the numerous fractures and cool depositing the minerals
Fluids then continue to circulate causing alteration of the initial ore deposit

## Slide 53: Bingham Pit
http://www.geomineinfo.com/mining_photos.htm
http://www.flickr.com/photos/johnbullas/2292342252/
http://www.geomineinfo.com/mining_photos.htm
http://earthobservatory.nasa.gov/IOTD/view.php?id=8144

## Slide 54: Outcrops
http://www.icmj2.com/03Mar/03MarFeature.htm
Gossan over depleted zone

## Slide 55: Mining & processing
http://www.flickriver.com/photos/earthworks/random/
http://electrochem.cwru.edu/encycl/art-m02-metals.htm
240 ton trucks
Tailings
ponds
Ball mills and flotation cells
Grade-0.25-2% Cu
+Au and Mo

## Slide 57: Cu production

## Slide 58: Lithium
Extracted primarily from pegmatites and brines

## Slide 59: Pegmatites
Plutonic intrusions
Coarse grain size
Extended fractional crystallisation of a fertile magma
Li-bearing pegmatites are relatively rare
Greenbushes Australia is the main worked pegmatite for lithium
Granitic pegmatite
K(Li,Al3)(AlSi3)O10(OH,F)2

## Slide 60: Continental brines
Occur in endorheic basins in areas with high evaporation rates
Cheaper and more efficient than mining rock
Key area is the central Andes –salt lakes and evaporite deposits
Source of Li thought to be the Puno-Altiplano magma body
Pumped out
Uses ~500,000 gallons of water per tonne of Lithium-env. Impact

## Slide 61: Lithium distribution

## Slide 63: Cobalt

## Slide 64: Cobalt
Ore minerals include:
  Cattierite CoS2
  Cobaltite CoAsS
  Erythrite Co3(AsO4)2·8H2O
CoS2

## Slide 65: Sediment-hosted copper deposits
Significant source of Cu
Cobalt grades in CACB vary from 0.1-1% Co

## Slide 66: Formation model for Sed-hosted Co-Cu belt deposits

## Slide 67: Cobalt
Cobalt mined from
  Ni-Laterites
  Ni-sulphide deposits
  Stratiform Cu-belt deposits

## Slide 68: Summary
Metals are essential for infrastructure, energy, and technology
Critical materials (e.g., lithium, cobalt, rare earth elements) are vital for the energy transition
Plate Tectonics influences resource distribution (e.g., mid-ocean ridges, subduction zones)
Key ore forming processes often involve precipitation from fluids
Growing demand for battery elements (Li, Ni, Co, Mn, Cu)
Wide range of ore deposit types, many host more than one economic metal

## Slide 70
PAPER OF THE WEEK

## Slide 71: The Raw Material Challenge of a Green Economy
Transition to a low-carbon economy demands significant mineral resources
Despite recycling efforts, new mining is necessary to meet demand.
Global mineral consumption will continue rising beyond 2050.

## Slide 72: Can Recycling or Waste Recovery Deliver Everything We Need?
Notes: Recycling and reprocessing of waste are essential but insufficient.

## Slide 73: Challenges and Solutions in Mineral Supply
Current mining lead time (~16 years) is too long to meet demand.

## Slide 75: A Sustainable Mining Future
Ethical and environmental concerns must be addressed.
Concept of ‘cradle-to-cradle’ mining to ensure net-positive impact.
Responsible mining can support the UN Sustainable Development Goals.
Balance between terrestrial and ocean mining must be considered.

## Slide 76: Discussion question
What are the biggest challenges in securing a mineral supply for a low-carbon future?